**Specifications**

Conforms to requirements of BS EN 15102,

BS EN 259 and Federal Specification

CCC-W-408A & C CFFA Quality Standard

for Vinyl Coated Fabric Wallcoverings

CFFA-W-101A

**Stain/Chemical Resistance:**

Pass ASTM D-1308-1987 Federal Spot Test.

Resistant to temporary staining of oils,

fats, mild acids and alkalis.

**Quality Assurance:**

All management systems and production

procedures comply with ISO 9001, the

internationally recognised Quality

Standard.

**Availability:**

Every product stocked in depth.

5.00pm deadline for next day delivery.

(UK only)

**Origin:**

Designed, coloured, manufactured and

stocked in the UK.

**Warranty:**

Newmor offers a five year warranty

against manufacturing defects.

Full details available on application.

**Samples:**

Larger samples are readily available on

request.

**Maintenance:**

Fully washable and in most cases products

can be scrubbed repeatedly to remove any

marks without damaging the product itself.

Most products are also able to withstand

the use of chlorine cleaning agents.

**Physical properties**

Total weight: 400gsm

Vinyl Weight: 360gsm

Substrate Type: 100% Woven Cotton

 Cotton Scrim

Substrate weight: 40gsm

**Roll size:**

1.3m x 30m

**Fire Rating:**

Class ‘O” to the requirements of Approved

Document B of the British Building

Regulations (Class 1, BS 476 part 7).

Euroclass B - s2, d0. Class A ASTM E-84

Tunnel Test. Tested in accordance

with Epiradiateur test NFP 92 501:

Adhered to cement board M1

Adhered to plasterboard M1

**Adhesive:**

Fabric backed vinyls - Newmor Heavy.

Varies with substrate - please enquire.

**Bacteria Resistance:**

Manufactured to include antimicrobial

protection as standard to help

in the control of fungi, actinomycetes

and bacteria.

**Light Fast:**

BS EN ISO 20105 min 6

**LRV**

Available on Request